Article

Role of Polymer Micelles in the Delivery of Photodynamic Therapy Agent to Liposomes and Cells

Laure Gibot, Maxime Demazeau, Véronique Pimienta, Anne-Françoise Mingotaud, Patricia Vicendo, Fabrice Collin, Nathalie Martins Froment, Stéphane Dejean, Benjamin Nottelet, Clément Roux, Barbara Lonetti

Figure S1. Representative Pheophorbide a (Pheo) fluorescence spectra and extrapolated intensity at 675 nm. The solutions were obtained by the addition of different amounts of (a) PEO-PCL and (b) PEO-PS micelles to a 2.10-8 M Pheo solution in PBS. The fluorescence intensity increases while adding progressively the copolymer as Pheo enters the micellar hydrophobic environment.

Figure S2. Absorbance spectrum of Pheophorbide a in various environments.

SI.I Life time measurements

Life time measurements were performed with a Fluorolog 3–2 iHR 320 spectrometer (Horiba, Japan). The fluorescence life times of Pheophorbide a loaded in the copolymer micelles were measured using pulsed LED at 371 nm (NanoLED-370, Horiba, Japan) as the excitation source. The instrument response at 371 nm was measured using a solution of silica nanospheres (80 nm) at 0.5 mg/mL (NanoXact Silica Nanospheres, nanoComposix, US). The sample response was measured at 675 nm. The ratio between the photon rate received by the sensor and the photon level emitted by the excitation source was kept to 2% by adjusting the slot openings. For all measurements, the signal is collected until a point reaches 4000 hits. The acquisition is done using DAS6 software (Horiba, Japan) and data processing using DataStation software (Horiba, Japan). Pheophorbide concentration in the samples was 1.5 10−5 M.

Figure S3. Fluorescence Intensity decay and fit residuals in the case of Pheophorbide in ethanol.

Figure S4. Fluorescence Intensity decay and fit residuals in the case of Pheophorbide encapsulated in PEO-PCL micelles.

Figure S5. Fluorescence Intensity decay and fit residuals in the case of Pheophorbide encapsulated in PEO-PS micelles.

Figure S6. Fluorescence Intensity decay and fit residuals in the case of Pheophorbide in PBS.

Figure 7. Fluorescence and aborbance spectra of Pheophorbide a and Rhodamine. (a) Fluorescence absorption and emission spectra of Pheophorbide a (Pheo) and Rhodamine showing the overlap between the fluorescence emission spectrum of rhodamine and absorption spectrum of Pheo; b) Fluorescence intensity of rhodamine labelled DOPC LUVs, Pheo loaded copolymer micelles and the mixture of rhodamine labelled LUVs and Pheo loaded copolymer micelles (ex = 560 nm). It shows that fluorescence emission of Pheo (peak at 675 nm) appears in the mixture of rhodamine labelled LUVs and Pheo loaded copolymer micelles (green curve) excited at the rhodamine excitation wavelength, while it is absent without rhodamine labelled LUVs (blue curve).

SI.II Determination of R0 distances for Rhodamine b, Pheophorbide a and NBD.

As is well described in many textbooks, for example in the recent FRET, from theory to application [2] , we used equation 1 to calculate the critical distances R0 at which FRET efficiency reaches 50 %.

| R0=0.0218κΦDn4⋅J16 | Equation 1 |
| --- | --- |

Where κ is the dipole-dipole interaction factor; ΦD is the fluorescence quantum yield of the donor in the absence of an acceptor; J is the overlap integral between the emission of the donor and the absorption of the acceptor; n is the refractive index of the medium.

J was calculated using ae 2.2 software from fluortools (www.fluortools.com).

We take the accepted average value of 2/3 for this κ. For the donor fluorophores, we use quantum yield values measured in ethanol. Rhodamine-b: ΦD = 0.7 (include reference); NBD: ΦD = 0.1 (from Mazeres et al Biophysical journal 2016).

Figure S8. Fluorescence intensities of DOPC-Rho LUVs and Pheo-loaded micelles mixtures. Decrease of the fluorescence intensity relative to rhodamine labelled LUVs( = 591 nm) undergoing FRET with (a) PEO-PCL micelles, (b) PEO-PS micelles, (c) Pheophorbide free in PBS.

SI.III Synthesis of rhodamine labelled PEO-PCL

Materials

α-methoxy,-hydroxyl poly(ethylene glycol) (PEG5k Mn = 5000 g/mol), stannous octoate (Sn(Oct)2, 92.5–100%), ε-caprolactone (CL, 97%), Rhodamine B isothiocyanate, trimethylamine and anhydrous N,N-Dimethylformamide were purchased from Sigma-Aldrich (St-Quentin Fallavier, France). Toluene was distilled over CaH2, and DMSO was dried over molecular sieves (4Å) prior to use. PEG was dried by an azeotropic distillation in dry toluene. ε-CL was dried over calcium hydride (CaH2) for 48 h at room temperature and distilled under reduced pressure.

Syntheses

Synthesis of PEG5k-b-PCL4k.

The amphiphilic PEG-b-PCL diblock copolymer was synthesized by ring opening polymerization (ROP) of ε-caprolactone in toluene at 100°C. -methoxy, -hydroxyl poly(ethylene glycol) (Mntheo = 5000 g/mol) and stannous octoate were used as initiator and catalyst, respectively.  In a typical procedure, to a solution of PEG5K (4 g, 0.8 mmol) in 25 ml of toluene in a schlenk tube, CL (3g, 26 mmol) and Sn(Oct)2 (0.120 ml, 0.4 mmol) were added. Following freeze-pump-thaw cycles, the reaction was allowed to proceed for 24 h at 100 °C in a nitrogen atmosphere. The reaction was stopped by the addition of a drop of hydrochloric acid at 37%. The product was precipitated in a large excess of cold diethyl ether. PEG-b-PCL was obtained by filtration and dried 24 h in vacuo at room temperature. Yield 87%

1H NMR (300 MHz, CDCl3): δ = 4.05 (t, CH2CH2OCO), 3.64 (m, OCH2CH2O), 3.34 (s, CH3O), 2.30 (t, COCH2CH2), 1.65 (m, COCH2CH2CH2CH2CH2O), 1.39 (m, COCH2CH2CH2CH2CH2O). Mn,SEC = 11800 g mol−1, Đ = 1.3. Mn,NMR = 9300 g mol−1

Synthesis of PEG5k-b-PCL4k-Rhodamine b

In a typical procedure, in a round bottom flask PEG5k-b-PCL4k (500 mg, 5.5 × 10−2 mmol), rhodamine B isothiocyanate (29.78 mg, 1 eq.) and an excess triethylamine (150 µL, 20 eq.) were dissolved in 3mL of anhydrous N,N-Dimethylformamide.  The mixture was bubbled with argon during 15 min through a rubber septum. The solution was then heated at 50°C and the reaction was carried out under stirring and argon atmosphere for 24h. The reaction medium was then evaporated to dryness under reduced pressure. The crude polymer was purified by solubilization in warm ethanol, followed by precipitation upon cooling in an ice bath. The precipitated polymer was centrifuged at 4500 rpm and −10 °C for 20 min. This purification was repeated twice more to yield a polymer without free rhodamine as shown by SEC analyses coupled with a fluorescence detector. The final copolymer was dried in vacuum overnight. Yield 50%. Mn,SEC = 9900 g mol−1, Đ = 1.17

Characterizations

Average molecular weights (Mn) and dispersities (Ð) were determined by size exclusion chromatography (SEC, Shimadzu prominence) using pre-column PLgel 5 µm (50 × 7.5 mm), two mixed medium columns PLgel 5 µm MIXED-C (300 × 7.8 mm), a Shimadzu RI detector 20-A and a Shimadzu Fluorescence detector RF-20A xs (λex : 555 nm, λem :570 nm) (40 °C thermostatic analysis cells). THF was the mobile phase with 1 mL.min-1 flow at 40 °C (column temperature). The polymer was dissolved in THF to reach 5 mg·mL−1 concentration, afterwards, solution was filtered through a 0.45 µm CHROMAFIL® Xtra PTFE filter before injection. Mn and Ð were expressed according to calibration using polyethylene glycol standards. LabSolution Lite was used as the software.

1H NMR spectra were recorded using an AMX Brucker spectrometer operating at 300 MHz at room temperature. The solvent used was CDCl3. The chemical shift was expressed in ppm with respect to tetramethylsilane (TMS).

Size-exclusion chromatographyanalyses (SEC).

Figure S9. Size Exclusion Chromatography. Trace for (a) PEO-PCL (refractive index detector) and rhodamine b labelled PEO-PCL (b) refractive index detector and (c) fluorescence detector.

Figure S10. Fluorescence spectra for mixtures of NBD-labelled liposomes and Rhodamine-labelled micelles. (a) NBD labelled DOPC liposomes (red curve) and NBD labelled DOPC LUVschallenged with different amounts of rhodamine labelled PEO-PCL micelles (green curves). Fluorescence intensity relative to rhodamine labelled PEO-PCL micelles ( = 578 nm, ex = 464 nm) increases when they are in presence of NBD labelled liposomes; (b) Fluorescence spectra rhodamine labelled PEO-PCL micelles (ex = 464 nm) used to correct the fluorescence values from a).

Figure S11. Chemical structures of oxidised DOPC. (a) DOPC-(OOH) (818.6 Da) and (b) DOPC-(OOH)2 (850.6 Da).

Figure S12. Area of the peaks in the mass spectra relatives to DOPC (red curve), DOPC-(OOH) (blue curve) and DOPC-(OOH)2 (green curve) as a function of irradiation time and fitted curves in the case of (a) PEO-PCL micelles and (b) PEO-PS micelles.

Figure S13. HCT-116 tumor cell viability. It was quantified by Prestoblue assay after 24h of incubation with empty PEO-PCL and PEO-PS micelles in non irradiated condition. n > 6. Statistical analysis by One-way ANOVA followed by Tukey's multiple comparisons test. ns = non-significant; * p > 0.05, **** p < 0.0001. Data are represented as the mean value ± SEM.

References

- Roeder, B.; Korth, O.; Herter, R.; Hanke, T.; Hoehne, W. Photophysical properties of pheophorbide-a in different carrier-systems. In Proceedings of the Photochemotherapy: Photodynamic Therapy and Other Modalities. International Society for Optics and Photonics 1996, 2625, 179–186.

- Medintz, I.L.; Hildebrandt, N. FRET-Förster resonance energy transfer: from theory to applications; Wiley-VHC, Weinheim, Germany, 2013.

|  | © 2020 by the authors. Licensee MDPI, Basel, Switzerland. This article is an open access article distributed under the terms and conditions of the Creative Commons Attribution (CC BY) license (http://creativecommons.org/licenses/by/4.0/). |
| --- | --- |